## Slide 1: Impulse Excitation Technique
Refractory Applications by Paul Bosomworth President/CEO BuzzMac International, LLC
Contact Info
Email: paul@buzzmac.com
Ph: +1 (603) 835-3180

## Slide 2
TAP BRICK
MEASURE
VIBRATIONS
RECORD & ANALYSE
(damping/elastic properties)
Impulse Excitation Technique (IET)*
*also known as ping test, resonant vibration, impact acoustic resonance, eigen frequency method…

## Slide 3
Research
Development
Quality Control
Process Control
Cost Saving
COMPLIES WITH ASTM E1876 & C1259…

## Slide 4
Research & Development: Example 1
Thermal Shock Testing of Magnesia Brick
A series of gel-bonded magnesia refractories* were water quenched through temperature differences DT. The Young’s modulus (E) was measured afterward using a resonant frequency method similar to IET.
*ethyl silicate (EA1-EA4), tetraisoproplyl titanate (T-T), and a pressed brick (PB)
A new parameter, Rst, was used to quantify the thermal stress damage resistances which correlated to the pore sizes of the refractories1
1 Based on Ph.D. Thesis by P.A. Bosomworth, Leeds University, Leeds, UK, 1986
‘’

## Slide 5
Research & Development: Example 2
Monitoring Elastic Properties During Firing
Green extruded cylinder of a quartz-porcelain mixture fired to 1100°C1
1 P. A. Bosomworth, " Monitoring the Elastic Properties of Green Ceramics during Firing," Ceramic Industry (February 2016) &
Igor Stubna, Frantisek Chmelık, Anton Trnık, Peter Sin, “Acoustic Emission Study of Quartz Porcelain during Heating up to 1150°C,” Ceram. Int., 38 6919–6922 (2012)
Unfired (green) ceramics can be tested using IET and the changes in elastic properties monitored during firing.
NOTE: Elastic properties can also be monitored during hydration and other processes because the test is nondestructive

## Slide 6
Quality Control
Reducing Production Costs of Magnesite-Chrome Brick1
Sonic velocity = 2 x length x frequency
Chart: Cold Crushing Strength (ccs) vs Sonic Velocity
| 29 | 31 | 28.8 | 64.3 | 37.9 | 24.8 | 38.800000000000004 | 42.7 | 55.8 | 51.6 | 32.1 | 60.7 | 49 | 32.4 | 50.2 | 57.3 | 52.7 | 21.8 | 54.9 | 47.8 | 57.8 | 56.7 | 41.1 | 29.9 | 28.2 | 50.8 | 32.4 | 60.1 | 50.8 | 44.4 | 52.6 | 34.1 | 61.4 | 44.5 | 51.2 | 45.3 | 30.6 | 51.2 | 61.2 | 46.3 | 33.200000000000003 | 21.7 | 51.2 | 31.6 | 49.1 | 27.5 | 32.800000000000004
 | 1472 | 1565 | 1569 | 2011 | 1755 | 1533 | 1914 | 1870 | 1915 | 1951 | 1994 | 1915 | 1910 | 1818 | 1956 | 1960 | 2013 | 1735 | 2003 | 1942 | 1984 | 2055 | 1900 | 1726 | 1826 | 2122 | 1716 | 2013 | 1864 | 1958 | 2038 | 1936 | 2008 | 1949 | 2293 | 2025 | 1838 | 1909 | 2124 | 1866 | 1664 | 1843 | 1917 | 1710 | 2015 | 1655 | 1403
Low strength population that we want to identify
Cold crushing strength testing is a much slower and therefore a more expensive test than sonic velocity testing using IET
1 Paul A. Bosomworth and Pierre-Alexis Anctil, "Using IET to Reduce Production Costs," Ceramic Industry, 10-11 (November 2009)

## Slide 7
Conclusions and Comments
Any question or comments, please contact me on linkedin.com/in/paul-bosomworth-78151514
IET is ideally suited to measuring the elastic and damping properties of refractories
IET can be used over a variety of testing environments (high/low temperatures, humidity…)
IET is fast, efficient and relatively low cost compared to destructive mechanical testing
IET is suited to R&D, QC/QA, cost reduction…